Brekke Testing Laboratories, Duluth, Minnesota

Transmittal of the acceptance summary, project 2417, Harbor View Parking Structure, July 2026 placements

To: Ingrid Halloran, P.E., Sandvik Halloran Engineers, engineer of record. Copy: Priya Raman, Carlow Program Management, owner's representative. From: Gunnar Brekke, laboratory manager. Date: September 3, 2026.

Enclosed is the acceptance summary for the concrete placed on project 2417 in July 2026, prepared under 3.12.1 of Section 03 30 00. The last 28 day cylinders from the July sets were broken on August 28, and every cylinder strength in the summary was computed from the break record.

Both mixtures met 3.11.1 for the month. No strength test fell below the specified strength by more than the allowance in criterion (b), and no moving average of three fell below the specified strength. The tables below list the July sets of each mixture in the order their samples were molded. The averages beside the first tests of each mixture run on from the June tests, as the averages of each month do from the month before.

# M-4000, elevated decks, ramp slabs, stair landings and curbs

| Set | Cast | Placement | Strength test, psi | Moving average of three, psi | Status |
| --- | --- | --- | --- | --- | --- |
| S-088 | 07/09/2026 | Level 1 deck bay C | 4,280 | 4,283.3 | Used for acceptance |
| S-089 | 07/13/2026 | Level 1 deck bay D | 4,390 | 4,296.7 | Used for acceptance |
| S-090 | 07/16/2026 | Ramp slab east lower run | 4,190 | 4,286.7 | Used for acceptance |
| S-091 | 07/21/2026 | Ramp slab east upper run | 4,460 | 4,346.7 | Used for acceptance |
| S-092 | 07/23/2026 | Level 1 crossover | 4,240 | 4,296.7 | Used for acceptance |
| S-094 | 07/28/2026 | Level 1 stair landings | 4,310 | 4,336.7 | Used for acceptance |
| S-095 | 07/30/2026 | Level 1 ramp transition | 4,150 | 4,233.3 | Used for acceptance |
| S-096 | 07/31/2026 | Level 1 curbs and islands | 4,020 on one cylinder |  | Not used, incomplete test |

# M-6000, columns and shear walls

| Set | Cast | Placement | Strength test, psi | Moving average of three, psi | Status |
| --- | --- | --- | --- | --- | --- |
| S-188 | 07/14/2026 | Columns Level 1 grid 5 to 8 | 6,270 | 6,166.7 | Used for acceptance |
| S-189 | 07/20/2026 | Columns Level 1 grid 9 to 12 | 6,090 | 6,146.7 | Used for acceptance |
| S-190 | 07/22/2026 | Elevator pit walls | 6,190 | 6,183.3 | Used for acceptance |
| S-191 | 07/27/2026 | Columns Level 1 grid 13 to 16 | 5,640 at 29.3 days |  | Not used, outside the age tolerance |
| S-192 | 07/29/2026 | Shear walls stair 2 base lift | 5,960 | 6,080.0 | Used for acceptance |

# Notes to the July summary

Set S-096 lost one of its two 28 day cylinders in handling at the laboratory, and the set was reported as an incomplete test. The one cylinder is given for information. The curb placement of July 31 was the only M-4000 placement of that day, so the day is carried in the summary as sampled short of 3.10.1.

Set S-191 was broken at 29.3 days because the technician was held at another project on its date. It is reported with its age and was not used for acceptance. The column placement of July 27 is carried as sampled short for the same reason.

Set S-093 was voided in the field on July 24 when the molds were knocked over before the concrete had set, and no cylinders from it reached the laboratory. A second sample was taken from the next truck of the same placement, and its set is in the table above.

Slump, air content and concrete temperature were inside the limits of 2.4 on every July sample except the air content of set S-090, which read 7.7 percent against the upper limit of 7.5 percent. It is noted in the summary under 3.12.2.

The summary for the August and September placements will follow when the last of the September sets has reached 28 days, which is October 8. The laboratory will issue the two months as one summary, as your office asked, so that the Level 2, Level 3 and Level 4 decks are reported together.

The moving averages in the tables are carried to one decimal place, as the laboratory's procedure requires, and each is compared with the specified strength as carried. The cylinders behind every July test are listed on the break record that accompanies the summary, with the two measured diameters and the load of each.

Please call this office with any question on the enclosed summary. The break record and the field reports behind it are available for your review at the laboratory.